# 6711RE	RESENE ENVIRONMENTAL PAINTING EXTERIOR

## 1.	GENERAL

If you have pre-customised this work section using the "questions and answers" provided as part of the downloading process, it may be necessary to amend some clauses to suit the final project-specific version.

The section must still be checked and customised to suit the project being specified, by removing any other irrelevant details and adding project-specific details and selections.

This section relates to the surface preparation, painting and clear finishing of new and existing exterior substrates using Resene environmental architectural and decorative coating systems.

Modify or extend the above description to suit the project being specified.

This 6711RE RESENE ENVIRONMENTAL PAINTING EXTERIOR section is intended to be combined as appropriate with the sections listed below and they collectively comprise painting work:

-	6700R RESENE PAINTING GENERAL

-	6721RE RESENE ENVIRONMENTAL PAINTING INTERIOR

-	( or 6721R RESENE PAINTING INTERIOR )

These sections have been written for use with Resene Surface Information & Preparation Data Sheets (SIPDS) and online technical product data sheets.  Modify and extend the selected systems (refer to SELECTIONS) as necessary for the substrate and its particular location (e.g. the substrate may be the same for bathroom and bedroom but the finish may differ).

Add project-specific clauses where extensive masking and spraying of coatings is involved.  Add clauses when specifying spray or roller-applied high-build products, or when specifying heavy-duty and solid vinyl wallcoverings.

For specific technical information call the Resene Technical Helpline 0800 RESENE (0800 737 363) or at www.resene.co.nz

### 1.1	RELATED WORK

Refer to 6700R RESENE PAINTING GENERAL for general matters related to painting work.

Refer to 6721RE RESENE ENVIRONMENTAL PAINTING INTERIOR for interior paint systems.

Modify or delete, include cross references to other sections where these contain related work.  Other related sections in Masterspec Standard could be 6745R RESENE PROTECTIVE COATINGS - STEELWORK for protective coatings.

## 2.	PRODUCTS

Materials

### 2.1	PAINT TYPES GENERALLY/ THINNERS AND ADDITIVES

Refer to 6700R RESENE PAINTING GENERAL for product clauses.

Modify or extend, including adding clauses to this section where product information relates exclusively to exterior painting.

## 3.	EXECUTION

Conditions

### 3.1	EXECUTION

Refer to 6700R RESENE PAINTING GENERAL for execution clauses.

Modify or extend, including adding clauses to this section where product information relates exclusively to exterior painting.

## 4.	SELECTIONS

For further details on selections go to www.resene.co.nz.

Substitutions are not permitted to the following, unless stated otherwise.

If substitutions are permitted modify the statement above, ensure the NO SUBSTITUTIONS clause from GENERAL is treated the same.

Select the options to suit the project and delete options not specified.

### 4.1	CONTROL SAMPLES

| Location/substrate | Resene SIPDS number/system |
| --- | --- |
| ~ | ~ |

Use this clause where appearance is the main criteria.  The size and form of samples depend on the nature of the project.

### 4.2	SUPERVISED CONTROL SAMPLES

| Location/substrate | Resene SIPDS number/system |
| --- | --- |
| ~ | ~ |

Use this clause where both durability and appearance are important.

### 4.3	INSPECTION OF WORK

| Stage | Resene SIPDS Spec number/system |
| --- | --- |
| ~ | ~ |

The level of inspection will depend on the nature of the project and will range from full for large or complex projects, through to intermittent for straightforward work to occasional for initially establishing the standards of execution.

### 4.4	HARDWARE

Hardware for removal:	~

Paint system schedules

These suggested schedules may be included here.  However they may also be part of a finishes schedule located elsewhere in the specification, may be included on the drawings, or even documented separately.

### 4.5	EXTERIOR FINISHES

| Substrate | Resene SIPDS number | Colour |
| --- | --- | --- |
| Weatherboards | ~ | ~ |
| Timber Joinery/Fascias/Barges | ~ | ~ |
| Timber Deck | ~ | ~ |
| Concrete Masonry | ~ | ~ |

Dark colours may cause warping on unstable substrates. Resene 'CoolColour' technology reduces heat absorption of a wide range of colours. Contact your local Resene Representative or visit www.resene.co.nz for more information or visit www.resene.co.nz/coolcolour. Light reflectance values for Resene colours are available from www.resene.co.nz/colourlibrary.

Resene exterior paint systems

EXTERIOR PAINT SYSTEMS: Supply the listed Resene systems for the following substrates.

Note: Select the appropriate first coat by deleting those not applicable.

For a current list of VOC's for Resene products see

www.resene.co.nz/archspec/datashts/vocsummary.pdf.

For information on how to earn Green Star NZ points with paint see

www.resene.co.nz/greenstarnz.htm.

For a current list of Resene  Environmental Choice NZ approved paints see

www.resene.co.nz/comn/envissue/paintlst.htm.

Environmental exterior concrete

### 4.6	RESENE NEW EXTERIOR IN-SITU CONCRETE

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 3/1

1st coat	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where an Acrylic Weathertight membrane is required substitute 2nd & 3rd coats with:

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a Flat Mineral effect is required substitute 2nd & 3rd coats with:

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

3rd coat:	Resene AquaShield D601, Acrylic Mineral Effect

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team.  If required make contact via email - advice@resene.co.nz.

### 4.7	RESENE NEW EXTERIOR TILT SLAB/PRECAST CONCRETE

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1/1

1st coat	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All Form Oils and Release Agents must be removed from the surface prior to painting.

Refer to Resene SIPDS 3: 1/1 for surface preparation information.

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where an Acrylic Weathertight membrane is required substitute 2nd & 3rd coats with:

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a Flat Mineral effect is required substitute 2nd & 3rd coats with:

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

3rd coat:	Resene AquaShield D601, Acrylic Mineral Effect

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team. If required make contact via email - advice@resene.co.nz

### 4.8	RESENE NEW EXTERIOR CONCRETE BLOCK/MASONRY – WEATHERTIGHT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 2/1

1st coat	Resene X-200 D62, Acrylic Weathertight Membrane

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: applied as specified this system achieves >180 microns Dry Film Thickness.

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team.  If required make contact via email - advice@resene.co.nz.

### 4.9	RESENE NEW EXTERIOR CONCRETE BLOCK/MASONRY – NON - WEATHERTIGHT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 2/1

1st coat	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a standard acrylic Semi-Gloss coating is required substitute 2nd, & 3rd coats:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team.  If required make contact via email - advice@resene.co.nz.

### 4.10	RESENE NEW EXTERIOR CONCRETE RENDER/PLASTER

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 3/1

1st coat	Resene Limelock D809, Acrylic Cure & Seal

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: applied as specified this system achieves >180 microns Dry Film Thickness.

Where a standard acrylic Low sheen coating is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a standard acrylic Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where a Flat Mineral effect is required add 4th coat:

4th coat 	Resene AquaShield D601, Acrylic Mineral Effect

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team.  If required make contact via email - advice@resene.co.nz.

Environmental exterior timber

### 4.11	RESENE NEW EXTERIOR TIMBER, PLYWOOD, WEATHERBOARDS - UNPRIMED

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 1/1

1st coat	Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a Gloss finish is required substitute 2nd & 3rd coats with:

### 2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

3rd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information. www.resene.co.nz/coolcolour

### 4.12	RESENE NEW EXTERIOR TIMBER, WEATHERBOARDS – FACTORY PRIMED

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 2/1

1st coat	Resene Wood Primer D40, Solvent-borne Primer (NEC)

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

3rd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information. www.resene.co.nz/coolcolour

### 4.13	RESENE NEW EXTERIOR CEDAR WEATHERBOARDS - UNPRIMED

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 1/1

1st coat	Resene Wood Primer D40, Solvent-borne Primer (NEC)

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

3rd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information. www.resene.co.nz/coolcolour.

### 4.14	RESENE NEW EXTERIOR TIMBER JOINERY

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 7/1

1st coat	Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

2nd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

3rd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information www.resene.co.nz/coolcolour.

### 4.15	RESENE NEW EXTERIOR CEDAR JOINERY

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 7/1

1st coat	Resene Wood Primer D40, Solvent-borne Primer (NEC)

2nd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

3rd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information www.resene.co.nz/coolcolour.

### 4.16	RESENE NEW EXTERIOR TIMBER, CEDAR, PLYWOOD, WEATHERBOARDS - STAIN

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 4/1

1st coat	Resene Waterborne Woodsman D57a, Waterborne Stain

2nd coat:	Resene Waterborne Woodsman D57a, Waterborne Stain

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

If extra durability is required add a 3rd coat of:

3rd coat:	Resene Waterborne Woodsman D57a, Waterborne Stain

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information www.resene.co.nz/coolcolour.

Environmental galvanized steel roofing

### 4.17	RESENE NEW EXTERIOR BARE ZINC/GALVANIZED STEEL ROOFING - LESS THAN 6 MONTHS OLD

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 4/1

1st coat	Resene Galvo-Prime, Waterborne Galvanised Steel Primer

2nd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

3rd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: Where roof is within 500m of sea apply a second coat of the specified primer prior to topcoats.

Note: This section assumes the roofing is less than 6 months old.

Where solvent borne primer is required substitute 1st coat with:

Resene Galvo-One, Solvent borne Galvanised Steel Primer (NEC)

Where Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

3rd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered. Refer to the Resene Website for more information. www.resene.co.nz/coolcolour

Environmental fibre cement

### 4.18	RESENE NEW EXTERIOR FIBRE CEMENT CLADDING

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 4/1

1st coat	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where an acrylic weathertight membrane is required substitute 2nd & 3rd coats with:

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a Flat Mineral effect is required substitute 2nd & 3rd coats with:

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

3rd coat:	Resene AquaShield D601, Acrylic Mineral Effect

### 4.19	RESENE NEW EXTERIOR LINEA™ BOARDS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 4A/1

1st coat	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where an acrylic weathertight membrane is required substitute 2nd & 3rd coats with:

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a Flat Mineral effect is required substitute 2nd & 3rd coats with:

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

3rd coat:	Resene AquaShield D601, Acrylic Mineral Effect

### 4.20	RESENE NEW EXTERIOR FIBRE CEMENT SOFFITS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 4/1

1st coat	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Environmental PVC gutters

### 4.21	RESENE NEW EXTERIOR PVC GUTTERING, DOWNPIPES

Surface Prep:	Resene SIPDS No5 and Spec Sheet 5: 1/1

Primer:	Not required

1st coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information. www.resene.co.nz/coolcolour.