# 6711R	RESENE PAINTING EXTERIOR

## 1.	GENERAL

If you have pre-customised this work section using the "questions and answers" provided as part of the downloading process, it may be necessary to amend some clauses to suit the final project-specific version.

The section must still be checked and customised to suit the project being specified, by removing any other irrelevant details and adding project-specific details and selections.

This section relates to the surface preparation, painting and clear finishing of new and existing exterior substrates using Resene architectural and decorative coating systems.

Modify or extend the above description to suit the project being specified.

This 6711R RESENE PAINTING EXTERIOR section is intended to be combined as appropriate with the sections listed below and they collectively comprise painting work:

-	6700R RESENE PAINTING GENERAL

-	6721R RESENE PAINTING INTERIOR

-	6721RE RESENE ENVIRONMENTAL PAINTING INTERIOR

These sections have been written for use with Resene Surface Information & Preparation Data Sheets (SIPDS) and Resene's online product Technical Data Sheets..  Modify and extend the selected systems (refer to SELECTIONS) as necessary for the substrate and its particular location (e.g. the substrate may be the same for bathroom and bedroom but the finish may differ).

Add project-specific clauses where extensive masking and spraying of coatings is involved; especially where solventborne products are specified.  Add clauses when specifying spray or roller-applied high-build products, or when specifying heavy-duty and solid vinyl wallcoverings.

For specific technical information call the Resene Technical Helpline 0800 RESENE (0800 737 363) or at www.resene.co.nz

Related work

### 1.1	RELATED WORK

Refer to 6700R RESENE PAINTING GENERAL for general matters related to painting work.

Refer to 6721R RESENE PAINTING INTERIOR for interior paint systems.

Refer to 6721RE RESENE ENVIRONMENTAL PAINTING INTERIOR for interior paint systems.

Modify or delete, include cross references to other sections where these contain related work.  Other related sections in Masterspec Standard could be 6745R RESENE PROTECTIVE COATINGS - STEELWORK for protective coatings.

Requirements

### 1.2	SAMPLES

Refer to the general section 1270 CONSTRUCTION for details of how samples will be reviewed and how instructions to proceed will be given.  Provide the following samples for review:

|  | Sample A | Sample B | Sample C |
| --- | --- | --- | --- |
| Sample description: | ~ | ~ | ~ |
| Sample type: | ~ | ~ | ~ |
| Number: | ~ | ~ | ~ |
| Location: | ~ | ~ | ~ |
| Supporting documentation: | ~ | ~ | ~ |
| Reviewer: | Contract administrator ~ | Contract administrator ~ | Contract administrator ~ |
| Time for review: | 10 working days ~ | 10 working days ~ | 10 working days ~ |
| Review criteria: | ~ | ~ | ~ |

The intention of this clause is to allow samples to be obtained that are not otherwise readily available to a reviewer.

Delete rows and columns not required or add "n/a".

| Sample description: | Describe the sample, size etc. Prepare samples of the finished work as scheduled, including preparation and colour as specified. |
| --- | --- |
| Sample type: | Portable sample for review Portable control sample Fixed sample for review Fixed control sample Control samples define requirements for type and quality and are used for comparison purposes throughout the contract. A "portable" sample is a sample that is easily movable, convenient for carrying. A "fixed" sample is a sample (semi) permanently placed. Expand on these terms as necessary. |
| Number: | State number of samples required, e.g. a minimum of three control samples - portable allow a sample to be retained on site with the other samples retained by the contract administrator and contractor. |
| Location: | Identify location of fixed samples, e.g. off site, on site, in situ |
| Supporting documentation: | Describe any additional documents required to support the review. |
| Reviewer: | Modify to suit the project, add additional reviewers if required. |
| Time for review: | Alter time if required. Expand to state timing in relation to when and where the sample is provided, e.g. at first site meeting. |
| Review criteria: | For example: - Appearance - Texture - Colour Add any critical items. Provide clarity for work that is not dependent on the review to continue. |

## 2.	PRODUCTS

Materials

### 2.1	PAINT TYPES GENERALLY/ THINNERS AND ADDITIVES

Refer to 6700R RESENE PAINTING GENERAL for product clauses.

Modify or extend, including adding clauses to this section where product information relates exclusively to exterior painting.

## 3.	EXECUTION

Conditions

### 3.1	EXECUTION

Refer to 6700R RESENE PAINTING GENERAL for execution clauses.

Modify or extend, including adding clauses to this section where product information relates exclusively to exterior painting.

## 4.	SELECTIONS

Substitutions are not permitted to the following, unless stated otherwise.

### 4.1	INSPECTION OF WORK

| Stage | Resene SIPDS number/system |
| --- | --- |
| ~ | ~ |

The level of inspection will depend on the nature of the project and will range from full for large or complex projects, through to intermittent for straightforward work to occasional for initially establishing the standards of execution.  Refer to AS/NZS 2311 Appendix C, Inspection and Testing, for more background.

### 4.2	BACK PAINTING SCHEDULE

Paint 2 coats (including any pre-prime) to match exposed face coating.

| Cladding type | Extent of back painting |
| --- | --- |
| ~ | ~ |

Amend to suit project requirements

Extent options:	To cladding manufacturer's requirements

Bottom edge & 150mm up

Paint whole back, bottom & concealed edges of cladding

Paint cladding under trim before fixing

Paint whole back, bottom & concealed edges of trim

Note;

Some pre-finished cladding may still need back painting.

Paint, stain and clear finishes can have different sorts of requirements.

### 4.3	HARDWARE

Hardware for removal:	~

Paint system schedules

These suggested schedules may be included here.  However they may also be part of a finishes schedule located elsewhere in the specification, may be included on the drawings, or even documented separately.

### 4.4	EXTERIOR FINISHES

| Substrate | Resene SIPDS number | Colour |
| --- | --- | --- |
| Weatherboards | ~ | ~ |
| Timber Joinery/Fascias/Barges | ~ | ~ |
| Timber Deck | ~ | ~ |
| Concrete Masonry | ~ | ~ |

Dark colours may cause warping on unstable substrates. Resene 'CoolColour' technology reduces heat absorption of a wide range of colours. Contact your local Resene Representative or visit www.resene.co.nz for more information or visit www.resene.co.nz/coolcolour. Light reflectance values for Resene colours are available from www.resene.co.nz/colourlibrary.

Resene exterior paint systems

EXTERIOR PAINT SYSTEMS: Supply the listed Resene systems for the following substrates.

Note: Select the appropriate first coat by deleting those not applicable.

For a current list of VOC's for Resene products see www.resene.co.nz/archspec/datashts/vocsummary.pdf.

For information on how to earn Green Star NZ points with paint see

www.resene.co.nz/greenstarnz.htm.

For a current list of Resene Environmental Choice NZ approved paints see

www.resene.co.nz/comn/envissue/paintlst.htm

Exterior cementitious - new

### 4.5	RESENE NEW EXTERIOR IN-SITU CONCRETE

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1/1

1st coat	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where an acrylic weathertight membrane is required substitute 2nd & 3rd coats with:

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a Flat Mineral effect is required substitute 2nd & 3rd coats with:

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

3rd coat:	Resene AquaShield D601, Acrylic Mineral Effect

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team.  If required make contact by email - advice@resene.co.nz.

### 4.6	RESENE NEW EXTERIOR IN-SITU CONCRETE – WEATHERTIGHT MEMBRANE

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1/1

1st coat	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: applied as specified this system achieves >180 microns Dry Film Thickness.

Where a Flat Mineral effect is required add a 4th coat:

4th coat:	Resene AquaShield D601, Acrylic Mineral Effect

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team.  If required make contact by email - advice@resene.co.nz.

### 4.7	RESENE NEW EXTERIOR IN-SITU CONCRETE – HIGH BUILD ELASTOMERIC MEMBRANE

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1/1

1st coat	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene X-300E D64, High Build Elastomeric Membrane

3rd coat:	Resene X-300E D64, High Build Elastomeric Membrane

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: applied as specified this system achieves >270 microns Dry Film Thickness.

### 4.8	RESENE NEW EXTERIOR IN-SITU CONCRETE – PENETRATING WATER REPELLENT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3:1/1

Saturation coat:	Resene Solventborne Aquapel D65S, Water Repellent (NEC)

2nd coat:	Not Required

3rd coat:	Not Required

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

### 4.9	RESENE NEW EXTERIOR TILT SLAB/PRECAST CONCRETE

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1/1

1st coat	Resene ConcreteSeal 3in1 D409, Solvent-borne primer/sealer (NEC)

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where an acrylic weathertight membrane is required substitute 2nd & 3rd coats with:

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a Flat Mineral effect is required substitute 2nd & 3rd coats with:

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

3rd coat:	Resene AquaShield D601, Acrylic Mineral Effect

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team. If required make contact by email - advice@resene.co.nz.

### 4.10	RESENE NEW EXTERIOR TILT SLAB/PRECAST CONCRETE - WEATHERTIGHT MEMBRANE

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1/1

1st coat	Resene ConcreteSeal 3in1 D409, Solvent-borne primer/sealer (NEC)

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: applied as specified this system achieves >180 microns Dry Film Thickness.

Where a Flat Mineral effect is required add a 4th coat:

4th coat:	Resene AquaShield D601, Acrylic Mineral Effect

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team.  If required make contact by email - advice@resene.co.nz.

### 4.11	RESENE NEW EXTERIOR IN-SITU CONCRETE – CLEAR COAT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1C/1

Saturation coat: 	Resene Aquapel D65S, Solventborne Water Repellent

1st coat	Resene Concrete Clear Gloss D54a, Waterborne Glaze

2nd coat:	Resene Concrete Clear Satin D54a, Waterborne Glaze

3rd coat:	Resene Concrete Clear Satin D54a, Waterborne Glaze

Note: This clear system will not render the coated surface weathertight

Where Flat finish is required substitute 2nd & 3rd coats with:
2nd coat:Resene Concrete Clear Flat D54a, Waterborne Glaze
3rd coat:Resene Concrete Clear Flat D54a, Waterborne Glaze

Where Gloss finish is required substitute 2nd & 3rd coats with:
2nd coat:Resene Concrete Clear Gloss D54a, Waterborne Glaze
3rd coat:Resene Concrete Clear Gloss D54a, Waterborne Glaze

### 4.12	RESENE NEW EXTERIOR IN-SITU CONCRETE – ANTI-GRAFFITI CLEAR COAT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1C/1

Saturation coat:	Resene Aquapel D65S, Solventborne Water Repellent

1st coat	Resene Concrete Clear Gloss D54a, Waterborne Glaze

2nd coat:	Resene Uracryl GraffitiShield Semi-Gloss D58, Waterborne Anti-Graffiti

3rd coat:	Resene Uracryl GraffitiShield Semi-Gloss D58, Waterborne Anti-Graffiti

Note: Allow Resene Concrete Clear to dry for 48 hours prior to applying Resene Uracryl GraffitiShield

NOTE: This clear system will not render the coated surface weathertight.

Where Flat finish is required substitute 2nd & 3rd coats with:
2nd coat:Resene Uracryl GraffitiShield Flat D58, Waterborne Anti-Graffiti 
3rd coat:Resene Uracryl GraffitiShield Flat D58, Waterborne Anti-Graffiti

Where Gloss finish is required substitute 2nd & 3rd coats with:
2nd coat:Resene Uracryl GraffitiShield Gloss D58, Waterborne Anti-Graffiti 
3rd coat:Resene Uracryl GraffitiShield Gloss D58, Waterborne Anti-Graffiti

### 4.13	RESENE NEW EXTERIOR TILT SLAB/PRECAST CONCRETE – CLEAR COAT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1C/1

Saturation coat:	Resene Aquapel D65S, Solventborne Water Repellent

1st coat	Resene Concrete Clear Gloss D54a, Waterborne Glaze

2nd coat:	Resene Concrete Clear Satin D54a, Waterborne Glaze

3rd coat:	Resene Concrete Clear Satin D54a, Waterborne Glaze

NOTE: This clear system will not render the coated surface weathertight.

Where Flat finish is required substitute 2nd & 3rd coats with:
2nd coat:Resene Concrete Clear Flat D54a, Waterborne Glaze
3rd coat:Resene Concrete Clear Flat D54a, Waterborne Glaze

Where Gloss finish is required substitute 2nd & 3rd coats with:
2nd coat:Resene Concrete Clear Gloss D54a, Waterborne Glaze
3rd coat:Resene Concrete Clear Gloss D54a, Waterborne Glaze

### 4.14	RESENE NEW EXTERIOR TILT SLAB/PRECAST CONCRETE– ANTI-GRAFFITI CLEAR COAT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1C/1

Saturation coat:	Resene Aquapel D65S, Solventborne Water Repellent

1st coat	Resene Concrete Clear Gloss D54a, Waterborne Glaze

2nd coat:	Resene Uracryl GraffitiShield Semi-Gloss D58, Waterborne Anti-Graffiti

3rd coat:	Resene Uracryl GraffitiShield Semi-Gloss D58, Waterborne Anti-Graffiti

Note: Allow Resene Concrete Clear to dry for 48 hours prior to applying Resene Uracryl GraffitiShield. This system is not intended for polished or highly honed panels.

NOTE: This clear system will not render the coated surface weathertight.

Where Flat finish is required substitute 2nd & 3rd coats with:
2nd coat:Resene Uracryl GraffitiShield Flat D58, Waterborne Anti-Graffiti 
3rd coat:Resene Uracryl GraffitiShield Flat D58, Waterborne Anti-Graffiti

Where Gloss finish is required substitute 2nd & 3rd coats with:
2nd coat:Resene Uracryl GraffitiShield Gloss D58, Waterborne Anti-Graffiti 
3rd coat:Resene Uracryl GraffitiShield Gloss D58, Waterborne Anti-Graffiti

### 4.15	RESENE NEW EXTERIOR TILT SLAB/PRECAST CONCRETE - HIGH BUILD ELASTOMERIC MEMBRANE

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1/1

1st coat	Resene ConcreteSeal 3in1 D409, Solvent-borne primer/sealer (NEC)

2nd coat:	Resene X-300E D64, High Build Elastomeric Membrane

3rd coat:	Resene X-300E D64, High Build Elastomeric Membrane

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: applied as specified this system achieves >270 microns Dry Film Thickness.

### 4.16	RESENE NEW EXTERIOR TILT SLAB/PRECAST CONCRETE - PENETRATING WATER REPELLENT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1/1

Saturation coat:	Resene Solventborne Aquapel D65S, Water Repellent (NEC)

2nd coat:	Not Required

3rd coat:	Not Required

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

### 4.17	RESENE NEW EXTERIOR CONCRETE BLOCK/MASONRY- WEATHERTIGHT MEMBRANE

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 2/1

1st coat	Resene X-200 D62, Acrylic Weathertight Membrane

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: applied as specified this system achieves >180 microns Dry Film Thickness.

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team.  If required make contact by email - advice@resene.co.nz.

### 4.18	RESENE NEW EXTERIOR CONCRETE BLOCK/MASONRY - NON-WEATHERTIGHT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 2/1

1st coat	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a standard acrylic Semi-Gloss coating is required substitute 1st, 2nd, & 3rd coats:

1st coat	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team.  If required make contact via email - advice@resene.co.nz.

### 4.19	RESENE NEW EXTERIOR CONCRETE - RENDER/PLASTER

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 3/1

1st coat	Resene Limelock D809, Acrylic Cure & Seal

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a standard acrylic Low sheen coating is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a standard acrylic Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where a Flat Mineral effect is required add 4th coat:

4th coat	Resene AquaShield D601, Acrylic Mineral Effect

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team.  If required make contact by email - advice@resene.co.nz.

Exterior cementitious - existing

### 4.20	RESENE EXISTING EXTERIOR IN-SITU/TILT SLAB/PRECAST CONCRETE

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1/3

Spot prime:	Resene Sureseal D42, Solvent borne pigment sealer (NEC)

1st coat	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where an acrylic Weathertight Membrane is required substitute 1st & 2nd coats with:

1st coat:	Resene X-200 D62, Acrylic Weathertight Membrane

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a High Build Elastomeric Membrane is required substitute 1st & 2nd coats with:

1st coat:	Resene X-300E D64, High Build Elastomeric Membrane

2nd coat:	Resene X-300E D64, High Build Elastomeric Membrane

Where a Flat Mineral effect is required substitute 1st & 2nd coats with:

1st coat:	Resene AquaShield D601, Acrylic Mineral Effect

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team. If required make contact by email - advice@resene.co.nz.

### 4.21	RESENE EXISTING EXTERIOR CONCRETE BLOCK/MASONRY

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 2/3

Spot prime:	Resene Sureseal D42, Solvent borne pigment sealer (NEC)

1st coat	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where an acrylic Weathertight Membrane is required substitute 1st & 2nd coats with:

1st coat:	Resene X-200 D62, Acrylic Weathertight Membrane

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a High Build Elastomeric Membrane is required substitute 1st & 2nd coats with:

1st coat:	Resene X-300E D64, High Build Elastomeric Membrane

2nd coat:	Resene X-300E D64, High Build Elastomeric Membrane

Where a Flat Mineral effect is required substitute 1st & 2nd coats with:

1st coat:	Resene AquaShield D601, Acrylic Mineral Effect

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team. If required make contact by email - advice@resene.co.nz.

### 4.22	RESENE EXISTING EXTERIOR CONCRETE RENDER/PLASTER

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 3/3

Spot prime:	Resene Sureseal D42, Solvent borne pigment sealer (NEC)

1st coat	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where an acrylic Weathertight Membrane is required substitute 1st & 2nd coats with:

1st coat:	Resene X-200 D62, Acrylic Weathertight Membrane

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a High Build Elastomeric Membrane is required substitute 1st & 2nd coats with:

1st coat:	Resene X-300E D64, High Build Elastomeric Membrane

2nd coat:	Resene X-300E D64, High Build Elastomeric Membrane

Where a Flat Mineral effect is required substitute 1st & 2nd coats with:

1st coat:	Resene AquaShield D601, Acrylic Mineral Effect

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

Where Anti-Graffiti coatings are required please refer to the Resene Architectural & Specifier Services Team. If required make contact by email - advice@resene.co.nz.

Exterior timber - new

### 4.23	RESENE NEW EXTERIOR TIMBER, PLYWOOD, WEATHERBOARDS - UNPRIMED

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 1/1

1st coat:	Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

3rd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered. Refer to the Resene Website for more information. www.resene.co.nz/coolcolour.

### 4.24	RESENE NEW EXTERIOR TIMBER, WEATHERBOARDS - FACTORY PRIMED

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 2/1

1st coat:	Resene Wood Primer D40, Solvent-borne Primer (NEC)

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

3rd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information. www.resene.co.nz/coolcolour

### 4.25	RESENE NEW EXTERIOR CEDAR WEATHERBOARDS - UNPRIMED

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 1/1

1st coat:	Resene Wood Primer D40, Solvent-borne Primer (NEC)

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

3rd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information. www.resene.co.nz/coolcolour

### 4.26	RESENE NEW EXTERIOR TIMBER DOORS, JOINERY - UNPRIMED

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 7/1

1st coat:	Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

2nd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

3rd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

Where a Solvent borne enamel finish is required substitute:

2nd coat:	Resene Enamel Undercoat D44, general purpose undercoat (NEC)

3rd coat:	Resene Super Gloss D32, Solvent borne Gloss enamel (NEC)

4th coat:	Resene Super Gloss D32, Solvent borne Gloss enamel (NEC)

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information. www.resene.co.nz/coolcolour.

### 4.27	RESENE NEW EXTERIOR TIMBER DOORS, JOINERY – FACTORY PRIMED

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 8/1

1st coat:	Resene Wood Primer D40, Solvent-borne Primer

2nd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

3rd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

Where a Solvent borne enamel finish is required substitute:

2nd coat:	Resene Enamel Undercoat D44, general purpose undercoat

3rd coat:	Resene Super Gloss D32, Solvent borne Gloss enamel

4th coat:	Resene Super Gloss D32, Solvent borne Gloss enamel

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information. http://www.resene.co.nz/pdf/CoolColour.pdf

### 4.28	RESENE NEW EXTERIOR CEDAR DOORS, JOINERY - UNPRIMED

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 7/1

1st coat:	Resene Wood Primer D40, Solvent-borne Primer (NEC)

2nd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

3rd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

Where a Solvent borne enamel finish is required substitute:

2nd coat:	Resene Enamel Undercoat D44, general purpose undercoat

3rd coat:	Resene Super Gloss D32, Solvent borne Gloss enamel

4th coat: 	Resene Super Gloss D32, Solvent borne Gloss enamel

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information. www.resene.co.nz/coolcolour.

### 4.29	RESENE NEW EXTERIOR TIMBER, CEDAR, PLYWOOD, WEATHERBOARDS - STAIN

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 4/1

1st coat:	Resene Waterborne Woodsman D57a, Waterborne Stain

2nd coat:	Resene Waterborne Woodsman D57a, Waterborne Stain

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

If extra durability is required add a 3rd coat of:

3rd coat:	Resene Waterborne Woodsman D57a, Waterborne Stain

Where a Solvent borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Woodsman Wood Oil Stain D57, Solvent borne (NEC)

2nd coat:	Resene Woodsman Wood Oil Stain D57, Solvent borne (NEC)

If extra durability is required add a 3rd coat of:

3rd coat:	Resene Woodsman Wood Oil Stain D57, Solvent borne (NEC)

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information. www.resene.co.nz/coolcolour.

### 4.30	RESENE NEW EXTERIOR PINE TIMBER DECK

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 6/1

1st coat:	Resene Wood Primer D40, Solvent-borne Primer (NEC)

2nd coat:	Resene Walk-On Flooring & Paving Paint – D322, Waterborne

3rd coat:	Resene Walk-On Flooring & Paving Paint – D322, Waterborne

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a standard acrylic Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a Non-Skid finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Non-Skid Deck & Path, D313, Acrylic

3rd coat:	Resene Non-Skid Deck & Path, D313, Acrylic

### 4.31	RESENE NEW EXTERIOR HARDWOOD, KWILA, MERUBA DECK - STAIN

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 5/1

1st coat:	Resene Kwila Timber Stain D501, Solvent borne

2nd coat:	Resene Kwila Timber Stain D501, Solvent borne

Where a standard Solvent borne stain finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Woodsman Wood Oil Stain D57, Solvent borne

2nd coat:	Resene Woodsman Wood Oil Stain D57, Solvent borne

Exterior timber - existing

### 4.32	RESENE EXISTING EXTERIOR TIMBER, PLYWOOD, WEATHERBOARDS

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 1/3

Spot Prime:	 Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

1st coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Hi-Glo D31, Gloss Acrylic

2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered. Refer to the Resene Website for more information. www.resene.co.nz/coolcolour.

### 4.33	RESENE EXISTING EXTERIOR CEDAR WEATHERBOARDS

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 1/3

Spot Prime:	Resene Wood Primer D40, Solvent-borne Primer (NEC)

1st coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Hi-Glo D31, Gloss Acrylic

2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered. Refer to the Resene Website for more information. www.resene.co.nz/coolcolour.

### 4.34	RESENE EXISTING EXTERIOR TIMBER DOORS, JOINERY

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 7/3

Spot Prime:	Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

1st coat:	Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

2nd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

3rd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

Where a Solvent borne enamel finish is required substitute:

1st coat:	Resene Enamel Undercoat D44, general purpose undercoat (NEC)

2nd coat:	Resene Super Gloss D32, Solvent borne Gloss enamel (NEC)

3rd coat:	Resene Super Gloss D32, Solvent borne Gloss enamel (NEC)

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered. Refer to the Resene Website for more information. www.resene.co.nz/coolcolour

### 4.35	RESENE EXISTING EXTERIOR CEDAR DOORS, JOINERY

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 7/3

Spot Prime:	Resene Wood Primer D40, Solvent-borne Primer (NEC)

1st coat:	Resene Quick Dry D45, Waterborne Acrylic Primer Undercoat

2nd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

3rd coat:	Resene Lustacryl D310, Semi-Gloss Waterborne Enamel

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Gloss Waterborne Enamel

3rd coat:
	Resene Enamacryl D309, Gloss Waterborne Enamel

Where a Solvent borne enamel finish is required substitute:

1st coat:	Resene Enamel Undercoat D44, general purpose undercoat (NEC)

2nd coat:	Resene Super Gloss D32, Solvent borne Gloss enamel (NEC)

3rd coat:	Resene Super Gloss D32, Solvent borne Gloss enamel (NEC)

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered. Refer to the Resene Website for more information. www.resene.co.nz/coolcolour.

### 4.36	RESENE EXISTING EXTERIOR TIMBER, CEDAR, PLYWOOD, WEATHERBOARDS

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 4/3

1st coat:	Resene Waterborne Woodsman D57a, Waterborne Stain

2nd coat:	Resene Waterborne Woodsman D57a, Waterborne Stain

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Solvent borne finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Woodsman Wood Oil Stain D57, Solvent borne

2nd coat:	Resene Woodsman Wood Oil Stain D57, Solvent borne

### 4.37	RESENE EXISTING EXTERIOR PINE DECK

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 6/3

Spot Prime:	Resene Wood Primer D40, Solvent-borne Primer (NEC)

1st coat:	Resene Walk-On Flooring & Paving Paint – D322, Waterborne

2nd coat:	Resene Walk-On Flooring & Paving Paint – D322, Waterborne

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: this section assumes the existing coating is acrylic.  If it is a polyurethane paving/decking type an adhesion primer of Resene ConcreteSeal 3in1 D409 will be required to all existing polyurethane paint coating.

Where a standard acrylic Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a Non-Skid finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Non-Skid Deck & Path, D313, Acrylic

2nd coat:	Resene Non-Skid Deck & Path, D313, Acrylic

### 4.38	RESENE EXISTING EXTERIOR HARDWOOD, KWILA, MERUBA DECK

Surface Prep:	Resene SIPDS No2 and Spec Sheet 2: 5/3

1st coat:	Resene Kwila Timber Stain D501, Solvent borne

2nd coat:	Resene Kwila Timber Stain D501, Solvent borne

Where a standard Solvent borne stain finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Woodsman Wood Oil Stain D57, Solvent borne

2nd coat:	Resene Woodsman Wood Oil Stain D57, Solvent borne

Exterior zinc galvanized steel roofing - new

### 4.39	RESENE NEW EXTERIOR FACTORY COATED ZINC/GALVANISED STEEL ROOFING (LESS THAN 6 MONTHS OLD)

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 4/1

1st coat:	Resene Pre-Coated Steel Primer D413, Alkyd Primer

2nd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

3rd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: Where roof is within 500m of sea apply a second coat of the specified primer prior to topcoats.

Where Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

3rd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered. Refer to the Resene Website for more information. . http://www.resene.co.nz/pdf/CoolColour.pdf

### 4.40	RESENE NEW EXTERIOR BARE ZINC/GALV STEEL ROOFING (LESS THAN 6 MONTHS OLD)

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 4/1

1st coat:	Resene Galvo-Prime, Waterborne Galvanised Steel Primer (NEC)

2nd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

3rd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: This section assumes the roofing is less than 6 months old.

Note: Where roof is within 500m of sea apply a second coat of the specified primer prior to topcoats.

Where solvent borne primer is required substitute 1st coat with:

Resene Galvo-One, Solvent borne Galvanised Steel Primer (NEC)

Where Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

3rd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered. Refer to the Resene Website for more information. www.resene.co.nz/coolcolour.

### 4.41	RESENE NEW EXTERIOR BARE ZINC/GALV STEEL ROOFING (EXPOSED LONGER THAN 6 MONTHS)

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 4/2

1st coat:	Resene Galvo-One, Solvent borne Galvanised Steel Primer (NEC)

2nd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

3rd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Note: This section assumes the roofing is greater than 6 months old.

Note: Where roof is within 500m of sea apply a second coat of the specified primer prior to topcoats.

Where Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

3rd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered. Refer to the Resene Website for more information. www.resene.co.nz/coolcolour.

Exterior zinc galvanized steel roofing - existing

### 4.42	RESENE EXISTING EXTERIOR PAINTED ZINC/GALVANIZED STEEL ROOFING

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 4/3

Spot Prime:	Resene Galvo-One, Solvent borne Galvanised Steel Primer (NEC)

1st coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

2nd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where mild red rust is evident substitute Spot Prime with:

Resene GP Metal Primer D411, Modified Alkyd Primer (NEC)

Where Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Hi-Glo D31, Gloss Acrylic

2nd coat:	Resene Hi-Glo D31, Gloss Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered. Refer to the Resene Website for more information. www.resene.co.nz/coolcolour.

Exterior fibre cement cladding - new

### 4.43	RESENE NEW EXTERIOR FIBRE CEMENT CLADDING

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 4/1

1st coat:	Resene Concrete Primer D405, Acrylic Concrete Primer (NEC)

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where an acrylic weathertight membrane is required substitute 2nd & 3rd coats with:

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a Flat Mineral effect is required substitute 2nd & 3rd coats with:

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

3rd coat:	Resene AquaShield D601, Acrylic Mineral Effect

### 4.44	RESENE NEW EXTERIOR FIBRE CEMENT CLADDING – CLEAR COAT

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 4/C1

Saturation coat:	Resene Aquapel D65S, Solventborne Water Repellent

1st coat:	Resene Concrete Clear Gloss D54a, Waterborne Glaze

2nd coat:	Resene Concrete Clear Satin D54a, Waterborne Glaze

3rd coat:	Resene Concrete Clear Satin D54a, Waterborne Glaze

NOTE: This clear system will not render the coated surface weathertight.

Where Flat finish is required substitute 2nd & 3rd coats with:
2nd coat:Resene Concrete Clear Flat D54a, Waterborne Glaze
3rd coat:Resene Concrete Clear Flat D54a, Waterborne Glaze

Where Gloss finish is required substitute 2nd & 3rd coats with:
2nd coat:Resene Concrete Clear Gloss D54a, Waterborne Glaze
3rd coat:Resene Concrete Clear Gloss D54a, Waterborne Glaze

### 4.45	RESENE NEW EXTERIOR LINEA™ BOARDS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 4A/1

1st coat:	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where a Flat Mineral effect is required substitute 2nd & 3rd coats with:

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

3rd coat:	Resene AquaShield D601, Acrylic Mineral Effect

### 4.46	RESENE NEW EXTERIOR FIBRE CEMENT SOFFITS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 4/1

1st coat:	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 2nd & 3rd coats with

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Exterior fibre cement cladding - existing

### 4.47	RESENE EXISTING EXTERIOR FIBRE CEMENT CLADDING

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 4/3

Spot Prime:	Resene Concrete Primer D405, Acrylic Concrete Primer

1st coat:	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

### 4.48	RESENE EXISTING EXTERIOR LINEA™ BOARDS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 4A/3

Spot Prime:	Resene Concrete Primer D405, Acrylic Concrete Primer

1st coat:	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where an acrylic weathertight membrane is required substitute 1st & 2nd coats with:

1st coat:	Resene X-200 D62, Acrylic Weathertight Membrane

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a Flat Mineral effect is required substitute 1st & 2nd coats with:

1st coat:	Resene AquaShield D601, Acrylic Mineral Effect

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

### 4.49	RESENE EXISTING EXTERIOR FIBRE CEMENT SOFFITS

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 4/3

Spot Prime:	Resene Concrete Primer D405, Acrylic Concrete Primer

1st coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Exterior brick - new

### 4.50	RESENE NEW EXTERIOR UNGLAZED BRICK

Surface Prep:	Resene SIPDS No5 and Spec Sheet 5:2/1

1st coat:	Resene Concrete Primer D405, Acrylic Concrete Primer

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Where an acrylic weathertight membrane is required substitute 2nd & 3rd coats with:

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a Flat Mineral effect is required substitute 2nd & 3rd coats with:

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

3rd coat:	Resene AquaShield D601, Acrylic Mineral Effect

### 4.51	RESENE NEW EXTERIOR BRICK - CONCRETE RENDER

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 3/1

1st coat:	Resene Limelock D809, Acrylic Cure & Seal

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

3rd coat:	Resene AquaShield D601, Acrylic Mineral Effect

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where an acrylic weathertight membrane is required substitute 2nd & 3rd coats with:

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a standard acrylic Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a standard acrylic Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

### 4.52	RESENE NEW EXTERIOR BRICK - BAGGED

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3: 1/1

1st coat	Resene Sureseal D42, Solvent borne Pigmented Sealer (NEC)

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

3rd coat:	Resene AquaShield D601, Acrylic Mineral Effect

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where an acrylic weathertight membrane is required substitute 2nd & 3rd coats with:

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

3rd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a standard acrylic Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a standard acrylic Semi-Gloss finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

3rd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Exterior brick - existing

### 4.53	RESENE EXISTING EXTERIOR BRICK

Surface Prep:	Resene SIPDS No3 and Spec Sheet 3:2/3

Spot Prime	Resene Sureseal D42, Solvent borne Pigmented Sealer (NEC)

1st coat:	Resene AquaShield D601, Acrylic Mineral Effect

2nd coat:	Resene AquaShield D601, Acrylic Mineral Effect

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where an acrylic weathertight membrane is required substitute 1st & 2nd coats with:

1st coat:	Resene X-200 D62, Acrylic Weathertight Membrane

2nd coat:	Resene X-200 D62, Acrylic Weathertight Membrane

Where a standard acrylic Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lumbersider, Low Sheen Acrylic

2nd coat:	Resene Lumbersider, Low Sheen Acrylic

Where a standard acrylic Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

Exterior metal- new

### 4.54	RESENE NEW EXTERIOR GALVANIZED/ZINC COATED STEEL

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 2/1

1st coat	Resene GP Metal Primer D411, Solvent borne Modified Alkyd (NEC)

2nd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

3rd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a standard acrylic Low Sheen finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a waterborne Semi-Gloss Enamel finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Lustacryl D310, Semi-Gloss waterborne enamel

3rd coat:	Resene Lustacryl D310, Semi-Gloss waterborne enamel

Where a waterborne Gloss Enamel finish is required substitute 2nd & 3rd coats with:

2nd coat:	Resene Enamacryl D309, Gloss waterborne enamel

3rd coat:	Resene Enamacryl D309, Gloss waterborne enamel

For Resene High Performance 2 pack type systems refer to MasterSpec 6745R.

### 4.55	RESENE NEW EXTERIOR MILD STEEL - SHOP PRIMED

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 1/1

1st coat	Resene GP Metal Primer D411, Solvent borne Modified Alkyd (NEC)

2nd coat:	Resene GP Metal Primer D411, Solvent borne Modified Alkyd

3rd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

4th coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

Note: this section assumes the Steel has been primed with a standard single pack Zinc phosphate primer.

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a standard acrylic Low Sheen finish is required substitute 3rd & 4th coats with:

3rd coat:	Resene Lumbersider D34, Low Sheen Acrylic

4th coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a waterborne Semi-Gloss Enamel finish is required substitute 3rd & 4th coats with:

3rd coat:	Resene Lustacryl D310, Semi-Gloss waterborne enamel

4th coat:	Resene Lustacryl D310, Semi-Gloss waterborne enamel

Where a waterborne Gloss Enamel finish is required substitute 3rd & 4th coats with:

3rd coat:	Resene Enamacryl D309, Gloss waterborne enamel

4th coat:	Resene Enamacryl D309, Gloss waterborne enamel

For Resene High Performance 2 pack type systems refer to MasterSpec 6745R.

### 4.56	RESENE NEW EXTERIOR ALUMINIUM JOINERY

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 8/1

1st coat	Resene Armourcote 821 RA37, Waterborne Epoxy Primer

2nd coat:	Resene Uracryl 802 RA55W, Waterborne Urethane Acrylic Semi-Gloss

3rd coat:	Resene Uracryl 802 RA55W, Waterborne Urethane Acrylic Semi-Gloss

Where a solvent borne Semi-Gloss finish is required substitute 1st, 2nd & 3rd coats with:

1st coat:	Resene Armourcote 221 RA36, Epoxy Primer

2nd coat:	Resene Uracryl 402 RA55, 2 pack Urethane Acrylic Semi-Gloss

3rd coat:	Resene Uracryl 402 RA55, 2 pack Urethane Acrylic Semi-Gloss

Where a solvent borne Gloss finish is required substitute 1st, 2nd & 3rd coats with:

1st coat:	Resene Armourcote 221 RA36, Epoxy Primer

2nd coat:	Resene Uracryl 403 RA56, 2 pack Urethane Acrylic Gloss

3rd coat:	Resene Uracryl 403 RA56, 2 pack Urethane Acrylic Gloss

Where a solvent borne Low Sheen finish is required substitute1st, 2nd & 3rd coats with:

1st coat:	Resene Armourcote 221 RA36, Epoxy Primer

2nd coat:	Resene Uracryl 404 RA59, 2 pack Urethane Acrylic Low Sheen

3rd coat:	Resene Uracryl 404 RA59, 2 pack Urethane Acrylic Low Sheen

Exterior metal - existing

### 4.57	RESENE EXISTING EXTERIOR GALVANIZED/ZINC COATED STEEL

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 2/3

Spot Prime:	Resene GP Metal Primer D411, Solvent borne Modified Alkyd (NEC)

1st coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

2nd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a standard acrylic Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a waterborne Semi-Gloss Enamel finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lustacryl D310, Semi-Gloss waterborne enamel

2nd coat:	Resene Lustacryl D310, Semi-Gloss waterborne enamel

Where a waterborne Gloss Enamel finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Enamacryl D309, Gloss waterborne enamel

2nd coat:	Resene Enamacryl D309, Gloss waterborne enamel

For Resene High Performance 2 pack type systems refer to MasterSpec 6745R

### 4.58	RESENE EXISTING EXTERIOR COPPER SPOUTING

Surface Prep:	Resene SIPDS No4 and Spec Sheet 4: 9/3

Spot Prime:	Resene Vinyl Etch RA31, Solvent borne adhesion primer (NEC)

1st coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

2nd coat:	Resene Summit Roof Semi-Gloss D315s, Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where a standard acrylic Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Where a standard acrylic Semi-Gloss finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Sonyx 101 D30, Semi-Gloss acrylic

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss acrylic

Exterior PVC - new

### 4.59	RESENE NEW EXTERIOR PVC GUTTERING, DOWNPIPES

Surface Prep:	Resene SIPDS No5 and Spec Sheet 5: 1/1

Primer:	Not required

1st coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information. www.resene.co.nz/coolcolour

Exterior PVC - existing

### 4.60	RESENE EXISTING EXTERIOR PVC GUTTERING, DOWNPIPES

Surface Prep:	Resene SIPDS No5 and Spec Sheet 5: 1/3

Spot Prime:	Resene Quick Dry D45, Acrylic Primer Undercoat

1st coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

2nd coat:	Resene Sonyx 101 D30, Semi-Gloss Acrylic

All products in this section are ECNZ (Environmental Choice New Zealand) approved unless otherwise noted with NEC (Non-Environmental Choice)

Where Low Sheen finish is required substitute 1st & 2nd coats with:

1st coat:	Resene Lumbersider D34, Low Sheen Acrylic

2nd coat:	Resene Lumbersider D34, Low Sheen Acrylic

Note: Where dark colours are selected the use of Resene Cool Colour Technology should be considered.  Refer to the Resene Website for more information. www.resene.co.nz/coolcolour